## Slide 1: 面內磁場下1T相二碲化鉑約瑟夫森接面之電流－相位關係研究
Study of the Current–Phase Relation of a 1T-PtTe Josephson Junction Under an In-Plane Magnetic Field Student: Tao-Yi Hsu (徐道宜) Advisor: Dr. Kuei-Lin Chiu (邱奎霖 博士)

## Slide 2: Introduction
Outline

## Slide 3
Introduction
Research motivation
1T-PtTe (Type-II Dirac)
Theory
Josephson effect & CPR
Josephson diode effect

## Slide 4
Research Motivation

## Slide 5
Topological SC
Type-II Dirac semimetal PtTe proximitized by a superconductor
Platform for novel quantum transport (surface/edge states)
CPR
Direct probe of junction physics beyond simple
Harmonics encode transparency / Andreev bound states

## Slide 6
1T-PtTe: A Type-II Dirac Semimetal

## Slide 7
Crystal Structure:
  Layered Transition Metal Dichalcogenide (TMD).
  CdI-type trigonal structure ().
  Te-Pt-Te tri-layers bound by van der Waals forces.
Electronic Properties:
  Type-II Dirac Fermions: Lorentz-invariance violating tilted Dirac cones.
  High conductivity and potential topological surface states (TSS).
Crystal structure of PtTe.

## Slide 8: Theoretical Background
Josephson Effect & Current–Phase Relation

## Slide 9
Josephson relations
DC: (ideal tunnel junction)
AC:
Beyond sinusoidal CPR
High transparency → skewed CPR
Harmonics:
Access via asymmetric SQUID readout

## Slide 10
Josephson Diode Effect (Concept)

## Slide 11
Definition
Non‑reciprocal critical current
Superconducting rectification without Joule heating
Typical ingredients
Broken inversion symmetry + broken time‑reversal symmetry
Often tuned by with strong spin–orbit coupling

## Slide 12: Theoretical Model: Rashba + Zeeman
Rashba + Zeeman: Why We Care
Platform: 2D electron system at an interface (e.g. PtTe surface / S–PtTe junction)
Key ingredients:
  Strong spin–orbit coupling (SOC) → Rashba effect
  External magnetic field → Zeeman effect
Combined effect:
  Generates helical spin–momentum locking + spin splitting
  Breaks inversion and time-reversal symmetries → allows finite-momentum pairing and Josephson diode effect (JDE)
Minimal 2D Model (Rashba + Zeeman)
Momentum in plane:
Spin Pauli matrices:
Total Hamiltonian:
We will discuss:
  : Free 2D electron gas
  : Rashba spin–orbit coupling
  : Zeeman coupling to external magnetic field
Free 2D Electron Gas ()
Hamiltonian:
Symmetries:
  Time-reversal symmetry (TRS): preserved
  Inversion / mirror symmetry (including ): preserved if structure is centrosymmetric
  Spin SU(2) symmetry: full spin-rotation invariance
  In-plane rotational symmetry (if effective mass isotropic): approx. preserved
Physical picture:
  Spin-degenerate parabolic bands
  No spin–momentum locking; spin and momentum are independent
Rashba Term (): Origin and Form
Requires structural inversion asymmetry (SIA) + strong SOC
Rashba Hamiltonian:
Parameters:
  : Rashba coupling strength interfacial electric field
Physical effect:
  Spin–momentum locking in the plane:
    Spin lies in-plane and perpendicular to momentum
  Splits the spin-degenerate Fermi surface into two helically polarized Fermi circles
Rashba: Symmetry Breaking
Breaks structural inversion symmetry (SIA):
  Under : interfacial electric field changes sign
  Rashba coupling changes sign → is not inversion-invariant
Breaks full spin SU(2) symmetry:
  Spin no longer freely rotates; spin orientation is tied to momentum direction
  Only combined spin–orbital rotations may remain as approximate symmetries
Preserves time-reversal symmetry (TRS):
  Under : ,
  → TRS holds
  Kramers degeneracy: states at and remain degenerate
Zeeman Term (): Origin and Form
External magnetic field couples to spin:
Examples:
  In-plane field along : .
Physical effects:
  Spin-splitting of bands
  Polarization of spins along
  Modifies Fermi surfaces for spin-up and spin-down differently
Zeeman: Symmetry Breaking
Breaks time-reversal symmetry (TRS):
  Magnetic field is odd under time reversal
  With , the system is no longer invariant under
  Lifts Kramers degeneracy
Reduces spin SU(2) to U(1):
  Only spin rotations about the axis remain symmetric
  Spin is preferentially aligned parallel or antiparallel to
Spatial symmetries:
  Depending on the crystal, selects a preferred axis
  May break certain rotational or mirror symmetries (e.g. in-plane mirrors) depending on direction of
Rashba + Zeeman Together
Combined Hamiltonian:
Symmetry summary:
  Inversion symmetry (along ): broken by Rashba
  Time-reversal symmetry: broken by Zeeman (finite )
  Spin SU(2): strongly broken; only residual rotations around special axes
Physical consequences:
  Spin texture becomes helical + spin-split
  Fermi surfaces for opposite spins are shifted and distorted
  This structure is the microscopic origin of:
    finite-momentum Cooper pairing ()
    -shifted and second-harmonic CPR
    Josephson diode effect (JDE)
Connection to Finite-Momentum Pairing
In presence of Rashba + Zeeman:
  Spin–momentum locking: spin orientation tied to
  Zeeman shifts spin-split Fermi surfaces in momentum space
Result:
  Cooper pairs formed between time-reversed partners no longer centered at
  Effective pair momentum:
  e.g. for certain helical textures
In the Josephson junction:
  Additional phase:
  Appears in CPR as:
  This is the GL-level description used to model JDE in PtTe / NiTe junctions.
Symmetry & JDE (Summary)
Two key symmetry breakings for JDE / -junction:
  Inversion symmetry broken → Rashba SOC
  Time-reversal symmetry broken → Zeeman field
Rashba + Zeeman together:
  Generate helical spin–momentum locking + finite- pairing
  Lead to a CPR containing higher harmonics and phase shifts:
  Allow nonreciprocal critical current:
Take-home message:
  Rashba = inversion breaking + SOC
  Zeeman = time-reversal breaking
  Combination is the microscopic mechanism for JDE

## Slide 13: Experimental Methods
Device Fabrication Flow
Crystal Growth: Self-flux method (provided by Prof. C.S. Lue, NCKU).
Exfoliation: Mechanical exfoliation of PtTe flakes onto SiO/Si substrates.
E-beam Lithography (EBL):
  PMMA resist coating.
  Pattern definition for contacts and SQUID loops.
Metallization:
  Superconducting electrodes: Al (Aluminum) or Nb (Niobium).
  In-situ Ar ion milling to ensure transparent interfaces.
  E-beam evaporation & Liftoff.
Design: Asymmetric dc-SQUID geometry for CPR retrieval.
Measurement Setup

## Slide 14
Cryogenic system: Dilution refrigerator (base ~40 mK)
Electronics: low-noise filtering, 4-terminal measurement
Magnetic control: 3-axis vector magnet (precise and alignment)
Measurement Schematic

## Slide 15: Results: Basic Characterization
I-V Characteristics (DC Transport)
Typical IV Curve:
  Clear Superconducting branch ().
  Switching Current () and Retrapping Current ().
  Hysteretic behavior (underdamped junction).

## Slide 16
I-V Curve at Base Temp.
Observation:
  Sharp transition indicates high-quality junction.
  Finite resistance in normal state ().
  Excess Current observed at high bias High transparency interface.

## Slide 17
Fraunhofer Pattern (AC Josephson Effect)

## Slide 18
Field modulation: vs. out-of-plane
Pattern cues
  Regular lobes → initially uniform current distribution
  Deviations → non-uniformity / phase winding changes
Fraunhofer Pattern

## Slide 19: Results: Current-Phase Relation
CPR Retrieval Method
Asymmetric SQUID Technique:
  Large junction () // Small junction ().
  .
  Assumes and sinusoidal .
Math Model:
  : Fundamental component (conventional).
  : Second harmonic (4-periodic / ABS).
Measured CPR & Fitting

## Slide 20
Extracted CPR Waveforms
Key Findings:
  Skewed CPR: Deviation from pure sine wave.
  High ratio: Significant second harmonic component detected.
  Indicates presence of highly transparent Andreev Bound States (ABS).

## Slide 21: Results: In-Plane Magnetic Field Effect
Tunable CPR with In-Plane Field

## Slide 22
Applying modifies CPR shape
Suggests a phase shift () in higher harmonics
Correlates with emergence of the Josephson diode effect
CPR Evolution under In-Plane Field

## Slide 23
Josephson Diode Effect (JDE)
Definition: Non-reciprocal critical current ().
Mechanism:
  Inversion symmetry breaking (structural or field-induced).
  Time-reversal symmetry breaking (-field).
  Finite momentum Cooper pairs?
Result:
  Efficiency .
  Tunable by magnetic field angle and magnitude.

## Slide 24: Conclusion
Summary
Successful Fabrication:
  High-quality 1T-PtTe Josephson junctions and SQUIDs realized.
Anomalous CPR:
  Observed significant second harmonic () contribution.
  Direct evidence of high-transparency transport modes.
Magnetic Tuning:
  In-plane magnetic field effectively modulates the CPR and induces Josephson Diode Effect.
  Demonstrates potential for tunable superconducting logic and phase batteries.
Future Outlook
Optimization: Improving fabrication yield and interface control.
Material Exploration: Extending to other Weyl/Dirac semimetals.
Quantum Information: Integration into superconducting qubit circuits (e.g., as non-linear inductive elements).

## Slide 25: References