## Slide 1: Investigation of Current-Phase Relationship in 1T-Phase Platinum Ditelluride Josephson Junctions under In-Plane Magnetic Field
面內磁場下 1T 相二碲化鉑約瑟夫森接面之電流-相位關係研究 Tao-Yi Hsu (徐道宜)

## Slide 2: Introduction
Outline
Introduction
  Research Motivation
  Type-II Dirac Semimetal (1T-PtTe)
Theoretical Background
  Josephson Effect & CPR
  Josephson Diode Effect (JDE)
Experimental Methods
  Device Fabrication
  Measurement Setup
Results & Discussion
  Basic Characterization
  Current-Phase Relation (CPR) Analysis
  Magnetic Field Dependence
Conclusion
Research Motivation
Emerging Topological Materials:
  Integration of Type-II Dirac Semimetals (e.g., PtTe) with superconductors.
  Exploring novel quantum transport phenomena (e.g., topological protection, helical edge states).
Current-Phase Relation (CPR) Physics:
  Direct measurement of CPR harmonics () beyond standard sinusoidal form.
  Understanding the role of superconducting proximity effect in topological materials.
Superconducting Diode Effect:
  Investigating non-reciprocal transport () in symmetric/asymmetric structures.
  Potential for dissipationless superconducting electronics.
1T-PtTe: A Type-II Dirac Semimetal

## Slide 3
Crystal Structure:
  Layered Transition Metal Dichalcogenide (TMD).
  CdI-type trigonal structure ().
  Te-Pt-Te tri-layers bound by van der Waals forces.
Electronic Properties:
  Type-II Dirac Fermions: Lorentz-invariance violating tilted Dirac cones.
  High conductivity and potential topological surface states (TSS).
Crystal structure of PtTe.

## Slide 4: Experimental Methods
Device Fabrication Flow
Crystal Growth: Self-flux method (provided by Prof. C.S. Lue, NCKU).
Exfoliation: Mechanical exfoliation of PtTe flakes onto SiO/Si substrates.
E-beam Lithography (EBL):
  PMMA resist coating.
  Pattern definition for contacts and SQUID loops.
Metallization:
  Superconducting electrodes: Al (Aluminum) or Nb (Niobium).
  In-situ Ar ion milling to ensure transparent interfaces.
  E-beam evaporation & Liftoff.
Design: Asymmetric dc-SQUID geometry for CPR retrieval.
Measurement Setup
Cryogenic System: Dilution Refrigerator (DR)
  Base temperature: ~40 mK.
Electronics:
  Low-noise filtering.
  4-terminal measurement (Current bias, Voltage readout).
Magnetic Field Control:
  3-axis vector magnet.
  Precision alignment of In-plane field () and Perpendicular field ().
Measurement Schematic

## Slide 5: Results: Basic Characterization
I-V Characteristics (DC Transport)
Typical IV Curve:
  Clear Superconducting branch ().
  Switching Current () and Retrapping Current ().
  Hysteretic behavior (underdamped junction).

## Slide 6
I-V Curve at Base Temp.
Observation:
  Sharp transition indicates high-quality junction.
  Finite resistance in normal state ().
  Excess Current observed at high bias High transparency interface.

## Slide 7
Fraunhofer Pattern (AC Josephson Effect)
Magnetic Field Modulation:
  vs. (Out-of-plane field).
Pattern Analysis:
  Regular oscillation indicates uniform current distribution initially.
  Deviations suggest non-uniformity or phase winding changes.
Fraunhofer Pattern

## Slide 8: Results: Current-Phase Relation
CPR Retrieval Method
Asymmetric SQUID Technique:
  Large junction () // Small junction ().
  .
  Assumes and sinusoidal .
Math Model:
  : Fundamental component (conventional).
  : Second harmonic (4-periodic / ABS).
Measured CPR & Fitting

## Slide 9
Extracted CPR Waveforms
Key Findings:
  Skewed CPR: Deviation from pure sine wave.
  High ratio: Significant second harmonic component detected.
  Indicates presence of highly transparent Andreev Bound States (ABS).

## Slide 10: Results: In-Plane Magnetic Field Effect
Tunable CPR with In-Plane Field
Observation:
  Applying modifies the CPR shape.
  Induces a phase shift () in the second harmonic?
  Evidence of Josephson Diode Effect (JDE).
CPR Evolution under In-Plane Field
Josephson Diode Effect (JDE)
Definition: Non-reciprocal critical current ().
Mechanism:
  Inversion symmetry breaking (structural or field-induced).
  Time-reversal symmetry breaking (-field).
  Finite momentum Cooper pairs?
Result:
  Efficiency .
  Tunable by magnetic field angle and magnitude.

## Slide 11: Conclusion
Summary
Successful Fabrication:
  High-quality 1T-PtTe Josephson junctions and SQUIDs realized.
Anomalous CPR:
  Observed significant second harmonic () contribution.
  Direct evidence of high-transparency transport modes.
Magnetic Tuning:
  In-plane magnetic field effectively modulates the CPR and induces Josephson Diode Effect.
  Demonstrates potential for tunable superconducting logic and phase batteries.
Future Outlook
Optimization: Improving fabrication yield and interface control.
Material Exploration: Extending to other Weyl/Dirac semimetals.
Quantum Information: Integration into superconducting qubit circuits (e.g., as non-linear inductive elements).

## Slide 12: References